## Slide 1: DEHub FDM Testbed
11/15/2024
Ahmed Ben Sidhom
Electrical and Computer Engineering PhD candidate
Advisor: Dr. Antonios Kontsos
Director, Digital Engineering Hub (DEHub)​
Henry M. Rowan Foundation Professor ​
Dept. of Mechanical Engineering​
Dept. of Electrical Engineering (courtesy)​
Materials Science & Engineering (affiliated)​
Henry M. Rowan College of Engineering (HMRCOE)

## Slide 2: Introduction
3D printing represents a significant leap forward in additive manufacturing technology. Despite its promising capabilities, the printing process often encounters various challenges, leading to frequent failures. These issues, such as under extrusion, stringing, and spaghettification, are diverse and recurrent, significantly impeding the seamless execution of print jobs. Consequently, these common errors pose substantial hurdles to the reliability and efficiency of 3D printing technology. These deficiencies can be rectified by having a closed-loop monitoring system, that can see defects and adjust printing properties to remove this defect from the rest of the print.
Example of 3D-Printing Defects

## Slide 3: Proposed Solution
Improve quality control in 3D printing by integrating real-time image analysis and acoustic emission sensing, enhanced through machine learning techniques:
Detecting and classifying defects in 3D-printed parts by analyzing images captured during the printing process in real time.
Identifying defect occurrence during printing using an acoustic sensor attached to the nozzle, providing real-time feedback on potential issues.

## Slide 4: Proposed Solution
This approach leverages the strengths of each method to offer complementary insights into the print condition:
Camera-based Computer Vision: Allows us to detect visible defects, such as layer misalignment, surface irregularities, or unexpected material build-up. By analyzing these images in real time, we can identify anomalies that are visually detectable, providing a reliable, immediate indication of certain types of physical defects as they occur.
Acoustic Emission (AE) Sensors: Detect high-frequency sound waves generated by subtle changes within the material that might not be visible, such as micro-cracks or material stress. This acoustic data enables us to identify structural issues that are hidden from the camera’s view.
By combining these two methods, we gain a fuller picture of the 3D printing process. This dual approach allows for a more robust, non-destructive monitoring system that enhances reliability and print quality assurance.

## Slide 5: Proposed Solution
Tools
3D Printer : Creality Ender 3 Pro
Printer Type​ | Fused Deposition Modeling (FDM)​
Build Volume​ | 220 x 220 x 250mm​
Print Head​ | Single​
XY Axis Accuracy​ | 0.1 mm​
Max Print Speed​ | 180 mm/s​
Nozzle Diameter​ | 0.4 mm​
Consumables​ | 1.75mm PLA, TPU, ABS​
Layer Resolution​ | 0.1 - 0.4 mm​

## Slide 6: Proposed Solution
Camera: Logitech C270
Raspberry Pi4
Tools

## Slide 7: Proposed Solution
AE sensor: VS600-Z1
Tools
AE DAQ: Linwave

## Slide 8: Proposed Solution
OctoPrint
OctoRest
Tools
Octopi
Octoprint

## Slide 9: Proposed Solution
Anaconda/Python/TensorFlow, Keras, Pytorch, Numpy…
Tools

## Slide 10: Defect Generation for Training
The geometry used to test these errors was a set of two cylindrical pillars with a rectangular tower in the middle.
To simulate under-extrusion, the g-code was modified to reduce the extrusion rate.
Stringing errors were induced by increasing the printing temperature and disabling retraction in Cura.
Spaghettification errors were generated by instructing the printer to create layers in midair, causing the extruded plastic to lack support and form long curls across the print bed.
Proposed geometry

## Slide 11: Defect Generation for Training
Property​ | Value​
Layer Height ​ | 0.2mm​
Wall Count ​ | 2​
Top & Bottom Layers ​ | 4​
Infill ​ | %10​
Infill Pattern​ | Cubic​
Nozzle Temperature ​ | 200.0 °C ​
Build Plate Temperature​ | 60.0 °C ​
Flow​ | 100% ​
Speed​ | 50 mm/s​
Build Plate Adhesion Type ​ | Skirt ​
Skirt Line Count​ | 3​
The object was sliced in Cura using default settings, representing a standard configuration for many 3D printers

## Slide 12: Approach 1: Computer Vision
Data Labeling and splitting
Model Training and evaluation
YOLO5s results
Images are captured during the printing process to detect purposely created defects by altering the G code, then the collected data is used to train an object detection model YOLOv5s

## Slide 13: Approach 1: Computer Vision
Team accessible data handling tool

## Slide 14: Approach 1: Computer Vision
Techniques: Anchor Boxes
Results: Object detection
Architectures: CNNs

## Slide 15: Approach 1: Computer Vision
YOLO
Faster-RCNN

## Slide 16: Approach 1: Computer Vision
Deployment and Closed-loop setup
Upon detection, commands are sent through OctoPrint installed on a RaspberryPi to adjust printer settings dynamically, ensuring optimal print quality.

## Slide 17: Approach 1: Computer Vision
Deployment and Closed-loop setup
1. Training
printer
camera
Computer
images
Octoprint
anaconda
Python
Dataset
Opencv
Numpy
…….
Pytorch
YOLO: Training
YOLO.pt
RoboFlow: Labeling/preprocessing/augmentation/splitting
Cloud

## Slide 18: Approach 1: Computer Vision
Deployment and Closed-loop setup
2. Deployment
printer
camera
Raspberry PI4
images
OctoPi
Python
Opencv
Numpy
…….
Pytorch
YOLO.pt: Inference
OctoRest
Results

## Slide 19: Approach 1: Computer Vision
Deployment and Closed-loop setup

## Slide 20: Approach 2: Time Series
DenseNet results
Acoustic emission signals generated during the printing process are captured and analyzed to identify patterns associated with various defects. Feature extraction techniques are applied to the acoustic data, and a dense neural network is trained to classify those defects.
Feature extraction and Data Labeling
Model Training and evaluation

## Slide 21: Approach 2: Time Series
Data acquisition parameters setup

## Slide 22: Approach 2: Time Series
Data structures
Real-time capabilities

## Slide 23: Approach 2: Time Series
Cyber Physical System : edge device

## Slide 24: Approach 2: Time Series
Tabulated data
Time series Data
Images: Matrix data

## Slide 25: Approach 2: Time Series
Deep-Learning

## Slide 26: Approach 2: Time Series
Deployment and Closed-loop setup
Our proposed monitoring system is capable of detecting print defects and adjusting printing parameters to correct them by:
Modifying nozzle temperature
Adjusting flow rate
Pausing the print

## Slide 27: Approach 2: Time Series
Deployment and Closed-loop setup
printer
AE sensor
AE waves
anaconda
Python
Dataset
TensorFlow
Numpy
…….
Keras
Model: Training
Model.Keras
Labeling/preprocessing/Feature Extraction/splitting
1. Training
Linwave
Computer

## Slide 28: Approach 2: Time Series
Deployment and Closed-loop setup
printer
AE sensor
AE waves
anaconda
Python
TensorFlow
Numpy
…….
Keras
Model.Keras: Inference
Results
Feature Extraction
2. Deployment
Linwave
Computer
OctoRest
OctoPrint

## Slide 29: Approach 2: Time Series
Deployment and Closed-loop setup

## Slide 30: Time for a hands-on project 3D Printer Connectivity
Plug in AC Adapter (power brick) into a 120 Volt power outlet
Plug in Male USB-C head into Female USB-C port on the Raspberry Pi
Leave power switch in the “off” position as shown below
2. Plug in Male USB-A from the Logitech C-270 webcam to the top right Female USB-A port of the Raspberry Pi
3. (White cable) Plug in Male USB-A to the top left Female USB-A port of the Raspberry Pi Plug in Male Micro-USB head into the Female Micro-USB port of the Ender 3 V2 3D Printer
4. Plug in NEMA 5-15 plug into a 120 Volt power outlet Plug in male IEC320 C13 plug (opposite end of NEMA 5-15’s cable) into Female IEC320 C13 port of the Ender 3 V2 3D Printer Power on the Ender 3 V2 3D Printer by flipping the switch to “on” position as shown below

## Slide 31: Time for a hands-on project OctoPrint and Raspberry Pi Setup
Download Raspberry Pi Imager
Insert the micro SD card from your Raspberry Pi 4 into a micro SD to SD adapter, then insert into your computer (Do NOT format the SD card on your PC/laptop)
3. Open the Raspberry Pi Imager
Under the “CHOOSE DEVICE” window, select “Raspberry Pi 4”
Under “CHOOSE OS” select the options “Other Specific Purpose OS” > “3D printing” > “OctoPi” and then the “stable” version
Under “CHOOSE STORAGE“ select the option for the micro SD card inserted into the computer
4. Before clicking “NEXT” press “Ctrl + Shift + x” in order to open the “”Advanced options”
Under “Set username and password” enter a new password to use for the system user “pi”. This is not the password you’ll use for logging into OctoPrint, but instead the one that you’ll have to use to log into your Pi via SSH, should you ever need to
Due to the nature of Rowan’s internet setup, create a hotspot using a mobile device instead of using the network “RowanWifi”
Under “Configure wireless LAN” type in the name of the hotspot, which cannot have spaces or special characters, and input the password for the hotspot
Change the “Wireless LAN country” to “US”
Click “SAVE” and then “NEXT” to initiate the process of writing and verifying
5. Locating the IP Address of the Raspberry Pi
Connect both your computer and the Raspberry Pi to the same network, the hot spot setup in the previous step
Download/Install the advanced IP scanner
Search for devices on your network, and locate the Raspberry Pi
d. Copy the IP address of the Raspberry Pi and place into the web
6. Follow the steps outlined by the Octoprint Setup wizard

## Slide 32: Thank you for your attention! Questions?
kontsos@rowan.edu
bensid28@students.rowan.edu